HIGH-LUB FA 67-220		08/97/32

Longterm grease for high loads		page 1 of 1

Description

BECHEM-RHUS FA 67-220 is a mineral oil based lubricating grease with a lithium-calcium thickener and has been specifically designed as a longterm lubricating grease. It is equipped with specially selected additives to provide the required corrosion protection properties and to enable the product to perform as a real longterm lubricant in a wide operating temperature range.

Service temperature range:					- 30 up to + 130°C,

Consistency acc. to DIN 51 818:				NLGI grade 2

Poss. denomination acc. to DIN 51 502:			KP 2 K - 30

Application

To lubricate heavily loaded roller bearings subjected to low or moderate speeds and, to provide longterm lubrication.

Characteristic data

Thickener							Li-Ca soap

Worked penetration				0,1 mm	280 +/- 15	DIN ISO 2137

Drop point					°C		approx. 175	DIN ISO 2176

Flow pressure at - 20°C			mbar		approx. 1200

Water resistance				rating		0 - 90		DIN 51 807,p.1

Oil separation, 7 days/40°C			%		approx. 2,5

Four Ball Test, weld load			N		3000		DIN 51 350,p.4

EMCOR corrosion test			rating		0 and 0	DIN 51 802

Copper corrosion, 24 h/120°C		rating		1		DIN 51 811

Mech.-dyn. tests:

FAG-FE 9, 120°C, F50			h		561		DIN 51 821

FAG-FE 8

n = 3000 rpm, n x dm = 285.000

c/p = 0,05 test time 500 h

wear on roll bodies , V 50		mg		31		DIN 51 821

Base oil :

Type								mineral oil

Kin. viscosity 40°C				mm²/s		approx. 220	DIN 51 562

Kin. viscosity 100°C				mm²/s		approx. 9,5	DIN 51 562

Flash point					°C		280		DIN ISO 2592

Pourpoint					°C		- 13		DIN 51 597

This information is intended as a guide and does not necessarily represent a marketing specification. Data may vary within modest ranges but do not adversely affect the lubricant quality. Modifications reserved. FA67220e.doc/Kenndaten/sk