BERUTOX FB 22			09/99/21

Multipurpose grease for			9012699

longlife lubrication				page 1 of 1

Description

To lubricate roller and plain bearings operating at high or low temperatues, vibrations, high load, high speeds as well as under open air conditions.

Service temperature range:				- 40 up to +180°C

Short term peak temperature				+ 200 °C

Consistency acc. DIN 51 818:			NLGI grade 2

Poss. denomination acc. DIN 51 502:		KPHC 2 R - 40

Benefits

To reduce friction, wear and to protect mechanisms against corrosion. BERUTOX FB 22 has excellent thermal stability. It is resistant to chemicals and performs as a real longlife lubricant at high loads.

Stops leaks at shaft seals in small-sized gears, keeps service temperatures low even at max. load. Suitable for very high temperature applications, BERUTOX FB 22 offers a maximum antiwear protection in a wide temperature range.

Examples of application

To lubricate roller and plain bearings, threaded spindles, toothed gears, worm gears exposed to severe variations in temperature and high load.

Characteristic data

Thickener						barium complex soap

Drop point			°C			appprox. 230		DIN ISO 2176

Worked penetration		0,1 mm		265 - 295		DIN ISO 2137

Water resistance					0 - 90			DIN 51 807

Apparent dyn. viscosity 25°C

gradient 300 s-1		mPa x s		approx. 5000		CB standard 0004

Low temperature properties							DB standard

at - 40°C (DB stirring test)	rating			3 (stirrable)		C1 StV 201

Flow pressure at - 35°C	mbar			< 550			DIN 51 805

Oil separation, 18 h/40°C	%			< 0,7			DIN 51 817

Base oil:

Type							synthetic oil

Kin. viscosity	40°C		mm²/s			approx. 50		DIN 51 562

Kin. viscosity	100°C		mm²/s			approx. 8		DIN 51 562

Flash point			°C			approx. 268		DIN ISO 2592

Pourpoint			°C			> - 65			DIN ISO 3016

This information is intended as a guide and does not necessarily represent a marketing specification. Data may vary within modest ranges but do not adversely affect the lubricant quality. Modifications reserved.