BERULIT GA 2500 FLUID	01/98/32

9006561

Open gear lubricant				page 1 of 1

Description

To lubricate large open gears. Suitable for bath lubrication or circulation systems.

Service temperature range:				+ 5 up to + 200°C

To reduce friction and wear on mechanisms subjected to mixed. friction. BERULIT GA 2500 Fluid offers excellent corrosion protection and absorbs vibrations.

Benefits

BERULIT GA 2500 Fluid is equipped with special EP additives and a selection of solid lubricants which enable the product to withstand high loads at high circumferential speeds up to approx. 8,5 m/sec such as at open gear drives in cement tube mills. BERULIT GA 2500 Fluid is specifically designed to be applied by bath lubrication or circulation systems.

Characteristic data

Thickener					Al complex soap

Worked penetration		0,1 mm	approx. 500		DIN ISO 2137

EMCOR corrosion test			0/0			DIN 51 802

Copper corrosion test				1			DIN 51 811

TIMKEN test

load		lbs		50			SEB 181 302

wear		mg		< 5

Four Ball Test								DIN 51 350 P. 4

O.K. load		N		8000

FZG test A/2,76/50							DIN 51 354

Damage load stage 			> 12

Specific wear		mgKWh	< 0,2

Base oil

Kin. viscosity 40°C		mm²/s		approx. 2500		DIN 51 562

Kin. viscosity 100°C		mm²/s		approx. 108		DIN 51 562

Flash point			°C		> 280			DIN ISO 2592

This information is intended as a guide and does not necessarily represent a marketing specification. Data may vary within modest ranges but do not adversely affect the lubricant quality. Modifications reserved.