BERULUB KRYOTOX EP 2	10/96/21

9012709

Low temperature and

high speed lubricant				page 1 of 2

Description

Synthetic low temperature and high speed lubricant of low internal friction. To lubricate plain and roller bearings usbjected to very low temperatures or high circumferential speeds.

Speed index (n x dm) = 106.

Service temperature range:				- 55 up to + 120°C

Consistency acc. DIN 51 818:			NLGI grade 2

Poss. denomination acc. DIN 51 502			KP E 2 K - 50

Reduces friction and wear, protects mechanisms from corrosion and abrasive buildup, helps prolong relubrication intervals.

Benefits

BERULUB KRYOTOX EP 2 is a real longterm lubricant and presents hardly any starting resistance at low temperatures. It is very beneficial to optical instruments, precision mechanisms or medical equipment. To be used whenever high speeds or low temperatures are involved.

Examples of application

To lubricate small-sized, miniature or high precision bearings. Also suitable for plain bearings, small-sized gears, electric motors and dental equipment operating at low driving power. Appropriate for bearings used in the cryogenic technology, textile machines, machine-tools, ski lifts and funiculars.

Characteristic data

Thickener						lithium hydroxystearate

Drop point				°C		195			DIN ISO 2176

Worked penetration			0,1 mm	265 - 295		DIN ISO 2137

Water resistance 					1 - 90			DIN 51 807

Copper corrosion test								DIN 51 811

80 °C/24 h			%		1

120°C/24 h			%		4

EMCOR corrosion					0 - 0			DIN 51 802

Oil separation,	18 h/40°C		%		0,4			DIN 51 817

7 days/40°C		%		2,0			DIN 51 817

TIMKEN test									SEB 181 302

load				lbs		45

wear				mg		< 3

# Flow pressure	+ 20°C			mbar		140		DIN 51 805

- 35°C			mbar		440			DIN 51 805

Apparent dyn. viscosity, 25°C							CB standard

gradient 300 s-1			mPa x s	approx. 4600

Deutsche Bahn stirring test - 45°C	rating		3, stirrable		DB standard

C 1 StV 201

BERULUB KRYOTOX EP 2	10/96/21

9012709

Low temperature and

high speed lubricant				page 1 of 2

Base oil

Type							synthetic oil

Kin .viscosity at 40°C			mm²/s		15			DIN 51 562

Kin. viscosity at 100°C		mm²/s		3,7			DIN 51 562

Flash point				°C		240			DIN ISO 2592

Pourpoint				°C		< - 60			DIN ISO 3016

Pack sizes

400 g cartridges - 1 kg metal tins - 5 kg pails - 10 kg pails - 25 kg kegs

This information is intended as a guide and does not necessarily represent a marketing specification. Data may vary within modest ranges but do not adversely affect the lubricant quality. Modifications reserved.