HIGH-LUB L 2MO			03/99/32

9004401

Longlife EP grease				page 1 of 1

Description

To lubricate roller and plain bearings exposed to shock load conditions and operating at a speed which still allows grease lubrication.

Service temperature range:				- 30 up to + 120°C

Consistency acc. to DIN 51 818			NLGI grade 2

Poss. denomination acc. DIN 51 502:		KPF 2 K - 30

To reduce friction and wear on industrial plain or roller bearings subjected mixed friction. HIGH-LUB L 2 MO is equipped with a specific portion of MoS2 and a selection of effective substances which give the product excellent EP and emergency run properties.

Examples of application

To lubricate drive shaft joints of knuckle joints.Also appropriate for bearings or joints such as used in rolling mills, machine tools, agricultural and constructional machinery, rail-road vehicles, caterpillar tractors, crushers, cranes, brake-rod linkages, eccentric bearings such as in jolters. Suitable as a for-life lubricant in small roller bearings used in electric motors, household appliances or electric units.

HIGH-LUB L 2 MO is also available in NLGI grade 3:

HIGH LUB L 3 MO		consistency acc. DIN 51 818:			NLGI grade 3

poss. denomination acc. DIN 51 502		KPF 3 K - 30

Characteristic data (of HIGH-LUB L 2 MO)

Thickener						Lithium/calcium soap

Drop point				°C		180			DIN ISO 2176

Worked penetration			0,1 mm	280  15		DIN ISO 2137

Penetration difference

between 60 000 / 60 DS		0,1 mm	< 30			DIN ISO 2137

Water resistance					1 - 90			DIN 51 807

EMCOR corrosion					0 - 0			DIN 51 802

TIMKEN test		load		lbs		43			SEB 181 302

wear		mg		< 5

This information is intended as a guide and does not necessarily represent a marketing specification. Data may vary within modest ranges but do not adversely affect the lubricant quality. Modifications reserved.