HIGH-LUB L 474 H

01/98/32

Longlife EP-grease			9004101

Page 1 of 1

Description

To lubricate roller and plain bearings as well as slideways subjected to high loads.

Service temperature range from - 20 up to + 120°C. Short term peak temperature to + 140°C.

Consistency acc.to DIN 51 818:			NLGI grade 2

Poss. denomination acc. to DIN 51 502:		KP 2 K - 20

Benefits

HIGH-LUB L 474 is equipped with excellent anti ageing and corrosion protection additves. Apart from this additives it contains special EP additives which improve the lubricating properties under heavy loads. HIGH-LUB L 474 H has very good adhesion.

Characteristic data

Thickener		Li-Ca-hydroxistearate

Drop point	0,1 mm	approx. 190	DIN ISO 2176

Worked penetration	0,1 mm	280 ± 15	DIN ISO 2137

Copper corrosion, 100°C/24 h		0	DIN 51 811

EMCOR corrosion test		0/0	DIN 51 802

TIMKEN test	load	lbs	43	SEB 181 302

wear	mg	< 5

Base oil

Type		mineral oil

Kin. viscosity 40°C	mm²/s	approx. 180	DIN 51 562

Flash point	°C	approx. 230	DIN ISO 2592

Pourpoint	°C	approx. - 20	DIN 51 597

This information is intended as a guide and does not necessarily represent a marketing specification. Data may vary within modest ranges but do not adversely affect the lubricant quality. Modifications reserved.