BERUTOX M 21 KN		09/96/32

9007601

High temperature grease			page 1 of 2

Description

To lubricate roller and plain bearings operating at high temperatures in a corrosive environment. Relubrication intervals and amounts of relubrication depend on operating conditions.

Service temperature range:				- 10 up to +180°C

Consistency acc. DIN 51 818:			NLGI grade 1 - 2

Poss. denomination acc. DIN 51 502:		KL 1,5 R - 10

To reduce friction and wear on mechanisms subjected to high temperatures and high loads and, to protect these against corrosion. To prevent the formation of abrasive buildup and ensure lubrication to be maintained also in the presence of water.

Benefits

BERUTOX M 21 KN holds its smooth texture without forming solid residues. When exceeding the indicated temperature range BERUTOX M 21 KN will form only very few residues. Relubricate as usual to maintain operational reliability. BERUTOX M 21 KN does not clog up pipings of central lubrication systems exposed to radiation heat up to + 260°C.

Oxidation and corrosion inhibitors in the grease provide reliable corrosion protection to prolong lifetime of mechanisms.

Owing to excellent temperature-consistency properties there will be just insignificant softening at high temperatures without affecting the product’s sealing properties.

Examples of application

To lubricate bearings exposed to severely high temperatures such as in annealing and drying furnaces, rotary kilns, manipulators, cooling beds, conveyor systems, hot air fans, certain electric motor types or waste gas fans for aggressive agents.

Characteristic data

Thickener						organic polymer

Drop opint			°C			> 250			DIN ISO 2176

Worked penetration		0,1 mm		300  10		DIN ISO 2137

Penetration difference								DIN ISO 2137

100 000 to 60 DS		0,1 mm		max. 40

Water resistance					1 - 90			DIN 51 807

Copper corrosion test 100°C/24 hrs			1			DIN 51 802

SKF R2F test rig								DIN 51 806

Test run at 180°C				passed

FAG FE 9 test rig								DIN 51 821

at 160°C, F50			hrs			310

FAG FE 8 test rig

150°C, n = 7,5 r.p.m.

p/c = 0,54 test time 500 hrs

roller body wear V50		mg			< 15

BERUTOX M 21 KN		09/96/32

9007601

High temperature grease			page 1 of 2

Base oil

Type							mineral oil

Kin. viscosity at 40°C		mm²/s			460			DIN 51 562

Kin. viscosity at 100°C	mm²/s			34			DIN 51 562

Flash point			°C			approx. 310		DIN ISO 2592

Pourpoint			°C			approx. - 15		DIN ISO 3016

This information is intended as a guide and does not necessarily represent a marketing specification. Data may vary within modest ranges but do not adversely affect the lubricant quality. Modifications reserved.