BERULUB SIHAF 2		03/99/21

9011309

Water tap grease				page 1 of 2

Description

BERLUB SIHAF 2 is a white silicone oil based speciality grease for hot and cold water taps as well as for other equipment and rubber seals such as used in breweries or the beverage industry.

Service temperature range:				- 40 up to + 160°C

Consistency acc. DIN 51 818:			NLGI grade 3

Poss. denomination acc. DIN 51 502			MSI 3 P - 40

To be used as a longlife grease for ceramic discs such as in water taps. To lubricate and seal stopcocks, rubber sleeves, special intake and discharge taps of machines such as used in breweries and the beverage industry.

Benefits

BERLUB SIHAF 2 is excellently resistant to water. It is a low maintenance product and keeps valves using aluminium oxide regulating discs tight and movable.

NOTE

BERULUB SIHAF 2 will not transmit odour or taste to drinking water and offers no health hazard. Complies with the hygiene requirements of the Federal Health Ofice („KTW“ recommendations with respect to the seal types D 1 and D 2).

Examples of application

Ensures operational reliability and improves the sliding ability of the metal-to-seal-contact such as EPDM/brass, -/bronze, -/aluminium, -/chromium and -/plastics.

BERULUB SIHAF 2 offers for-life lubrication of hot water taps, thermostatic valves and electrically controlled valves. BERULUB SIHAF 2 can also be used as a for-life lubricant for overflow valves such as used in electric hot water boilers.

Characteristic data

# Thickener						gel/solid lubricants

Drop point				°C		> 240			DIN ISO 2176

Worked penetration			0,1 mm	220 - 250		DIN ISO 2137

Water resistance					0 - 40			DIN 51 807

0 - 90

Oil separation after 18 h/90°C	%		< 0,5			with reference to

DIN 51 817

BERULUB SIHAF 2		03/99/21

9011309

Water tap grease				page 2 of 2

WRT grease test, loss in weight

after 1 h/90°C, 730 r.p.m.		%		no fling-off		CB standard

Apparent dynamic viscosity, 25°C

gradient 300 s-1			mPa x s	approx. 12 000	CB standard

Compatibility with plastics and			will not attack EPDM or NBR seals,

elastomers						generally compatible with conventional

plastics.

Base oil

Type							special silicone oil

Kin. viscosity at 40°C			mm²/s		approx. 1000		DIN 51 562

Kin. viscosity at 100°C		mm²/s		approx. 480		DIN 51 562

Flash point				°C		> 320			DIN ISO 2592

Pourpoint				°C		< - 50			DIN ISO 3016

Pack sizes

1 kg tins - 5 kg pails - 10 kg pails - 25 kg kegs - 50 kg kegs

This information is intended as a guide and does not necessarily represent a marketing specification. Data may vary within modest ranges but do not adversely affect the lubricant quality. Modifications reserved.