BECHEM STAROIL D EP-S	07/93

page 1 of 2

Description

Specially designed for the lubrication of guideways (to prevent stick-slip) and gears, bearings, bolts, spindles and other slideways such as in textile or paper machinery as well as in machine-tools.

BECHEM STAROIL D EP-S oils have good adhesion and excellent lubricating properties. The Protect mechanisms subjected to boundary friction against corrosion and do not drip off. BECHEM STAROIL D EP-S oils are equipped with a selection of effective substances which eleminate stick-slip of guideways at very low sliding or advance speeds. They have excellent demulsifying properties compared with cooling emulsions or solutions. Compatibility tests on BECHEM STAROIL D EP-S oils and coolants can be furnished upon request.

Characteristic data

|  |  | D 68 EP-S part no. 1501801 | D 220 EP-S part no. 1501901 |
| --- | --- | --- | --- |
| Classification acc. DIN 51 502 |  | CGLP 68 | CGLP 220 |
| Viscosity at 40°C | mm²/s | 68,21 | 214,3 |
| Viscosity at 100°C | mm²/s | 9,416 | 18,84 |
| Viscosity index |  | 116 | 98 |
| Pourpoint | °C | - 33 | - 27 |
| Density at 15°C | kg/m³ | 884,3 | 897,5 |
| Colour |  | 3,0 | 4,0 |
| Refractive index | nD20 | 1,4854 | 1,4931 |
| TBN | mgKOH/g | 0,19 | 0,19 |
| Saponification no. | mgKOH/g | 2,60 | 2,90 |
| Flash point, COC | °C | 232 | 253 |
| Turb.-corrosion test | rating | 0 | 0 |
| Copper strip test 100 A3 | rating | 1 | 1 |
| Demulsifying capacity, 54°C/15 min. | ml/ml/ml | 41/39/0 |  |
| Demulsifying capacity, 82°C/15 min. | ml/ml/ml |  | 42/38/0 |
| Air release capacity, 50°C | min. | 5 |  |
| Foam formation, sequence I | ml/ml/ml | 10/25/0 | 0/0/0 |
| Foam formation, sequence II | ml/ml/ml | 20/9/0 | 30/25/0 |
| Foam formation, sequence III | ml/ml/ml | 20/30/0 | 50/75/0 |
| Sulfide ash | % by weight | < 0,01 | < 0,01 |
| Oxide ash | % by weight | < 0,01 | < 0,01 |
| Brugger Test | N/mm²/s | 27,9 | 33,4 |
| FZG Test | load stage | > 12 | > 12 |
| Four Ball Test, 1 h/150 N, wear | mm | 0,14 | 0,22 |
| Four Ball Test, o.k./weld load | N | 1800/1900 | 2000/2100 |
| Tannert coefficient of friction |  | 0,23 | 0,14 |
| Tannert sliding index | N | 879 | 1744 |

BECHEM STAROIL D EP-S	07/93

page 2 of 2

| Swelling, SRE NBR 1 | volume % | + 6,4 | + 4,2 |
| --- | --- | --- | --- |
|  | Shore | - 3 | - 11,5 |
| Swelling, SRE NBR 28 | volume % | + 4,7 | + 2,4 |
|  | Shore | - 1,5 |  0 |
| Coefficient of friction (Schmidt method) | SKC 3 GG 25 | f0 = 0,079 | f0 = 0,079 |
|  | GG 25 - GG 25 | f0 = 0,157 | f0 = 0,170 |

This information is intended as a guide and does not necessarily represent a marketing specification. Data may vary within modest ranges but do not adversely affect the lubricant quality. Modifications reserved.