BECHEM STAROIL G	10/96/03

EP gear oils				page 1 of 1

Description

To be used for heavily loaded gear or worm gear drives, plain bearings or slideways such as used in steel or rolling mills, conveyor systems in coal and ore mining as well as in other industrial areas such as construction, earthmoving or paper mills.

Benefits

BECHEM STAROIL G EP gear oils are equipped with efficient antiwear additives and have excellent load carrying properties which make them also suitable as running-in oils. BECHEM STAROIL G EP gear oils are identified by very good aging resistance, excellent water and air release capacity, good viscosity-temperature properties and durable corrosion protection. BECHEM STAROIL G EP gear oils ensure operational reliability and prolong lifetime of gears even under extreme operating conditions.

Characteristic data

| STAROIL | Viscosity, 40°C, mm²/s | Viscosity, 50°C, mm²/s | Viscosity 100°C, mm2/s | Flash point °C, DIN 51584 | Pourpoint °C, DIN 51583 |
| --- | --- | --- | --- | --- | --- |
| G 46 part no. 800502 | 46,0  10 % | 30 | 6,9 | 220 | - 30 |
| G 68 part no. 800702 | 67,8  10 % | 42,6 | 8,8 | 225 | - 24 |
| G 100 part no. 9551601 | 100,5  10 % | 62 | 10,9 | 230 | - 24 |
| G 150 part no. 9551701 | 150,7  10 % | 88,6 | 14,8 | 230 | - 21 |
| G 220* part no. 9551901 | 220,0  10 % | 126 |  | 230 | - 18 |
| G 320 part no. 9553501 | 324,0  10 % | 176 |  | 235 | - 18 |
| G 460 part no. 9554501 | 460,0  10 % | 247 |  | 235 | - 15 |
| G 680 part no. 9555501 | 680,0  10 % | 375 |  | 240 | - 12 |

Vis. Index	Timken o.k. load	FZG Test A/80,3/90, DIN 51 354

DIN 51 563	(wear < 3 mg)		damage load stage	spec. wear

SEB 181 302

*STAROIL G 220:	> 90		> 50 lbs		> 12			< 0,2 mg/KWh

This information is intended as a guide and does not necessarily represent a marketing specification. Data may vary within modest ranges but do not adversely affect the lubricant quality. Modifications reserved.