BECHEM STAROIL No.	10/96

800902 / 800502

800202 / 800702

800302 / 800802

Hydraulic oils			page 1 of 1

Description

To be used as power transmission fluids for above all hydrostatically operated hydraulic plants subjected to thermal load, water ingress and possibly also corrosion. Appropriate for hydraulic pumps or motors which because of their design or operating conditions require antiwear additive-treated oils to protect mechanisms in the mixed friction area.

Benefits

Selected solvent-refined products and highly efficient additives have been combined to yield these oils which comply with all - even the severest - requirements. BECHEM STAROIL No. hyraulic oils are chemically stable. They are largely resistant to carbonization and will not form mud-like or acid products. They are equipped with excellent viscosity-temperature properties. When exposed to severer temperature variations, viscosity will change only slightly without affecting service reliability.

BECHEM STAROIL No. hydraulic oils are also identified by a good water and air release capacity. Air or water will not be emulsified but released within a very short time. Air escape valves and drainers help accelerate the process.

All mechanisms which are supplied with BECHEM STAROIL No. hydraulic oils are protected against the corrosive influences of air or humidity. Since BECHEM STAROIL No. hydraulic oils are neutral to seals, oil resistant seals will not be attacked and leakage is largely prevented.

Characteristic data

|  | No. 10 | No. 22 | No. 32 | No. 46 | No. 68 | No. 100 |
| --- | --- | --- | --- | --- | --- | --- |
| Classific. acc. DIN 51 502 | H-LP 10 | H-LP 22 | H-LP 32 | H-LP 46 | H-LP 68 | H-LP 100 |
| Density 15°C , g/ml | 0,862 | 0,864 | 0,870 | 0,874 | 0.878 | 0,880 |
| Viscosity, 40°C, mm²/s | 10,5  10 % | 22,0  10 % | 32,0  10 % | 46,0  10 % | 68,0  10 % | 100,0  10 % |
| Viscosity, 100°C, mm²/s | 2,7 | 4,4 | 5,5 | 6,9 | 8,80 | 10,5 |
| Flash point, °C | 159 | 205 | 215 | 220 | 250 | 250 |
| Pourpoint, °C | - 60 | - 40 | - 33 | - 27 | - 24 | - 18 |
| Air release cap. 50°C, min. | 4 | 4 | 6 | 10 | 12 | 19 |
| Water release cap. 54°C, min. | 15 | 15 | 25 | 30 | 40 | 50 |

BECHEM STAROIL No. hydraulic oils comply withthe requirements for H-LP hydraulic oils acc. to SEB 181 222, VDMA 24318 and DIN 51 524/2. Besides, they have proved successful in Vickers, Bühler or Hydromatic pumps.

This information is intended as a guide and does not necessarily represent a marketing specification. Data may vary within modest ranges but do not adversely affect the lubricant quality. Modifications reserved.