HIGH-LUB SW 2			12/98/21

9004372

Universal lubricant for mechanisms

exposed to saltwater atmosphere		page 1 of 3

Description

To lubricate roller and plain bearings subjected to mixed friction, to protect all sliding mechanisms especially wire ropes against corrosion and against the corrosive attack of aggressive waters or gases.

Service temperature range:					- 25 up to + 80°C

Application

To reduce friction and wear, to protect bearings from corrosion and to protect mechanisms against contamination especially in the presence of aggressive waters and moist gases.

Consistency acc. to DIN 51 818:			NLGI grade 2 - 1

Poss. denomination acc to DIN 51 502:		KPL 1,5 E - 25

# Complies with military spec.:			BW-TL 91050-066

Defence Standard 91-34/1

NATO G 460

Benefits

HIGH-LUB SW 2 protects all mechanisms subjected to friction against erosion and corrosion and is especially beneficial when these are exposed to seawater or seawater atmosphere. SW 2 is largely resistant to leaches or oxygenic acids. It makes mechanisms perfectly impermeable against ingress of hot or cold water and is thus the ideal lubricant whenever absolute water resistance is required.

HIGH-LUB SW 2 is equipped with a selection of additives and solid lubricants to give the product excellent EP and antiwear properties which are very beneficial in the area of mixed friction. HIGH-LUB SW 2 succesfully minimizes fretting corrosion.

Examples of application

To lubricate open gears, winches, screws, hinges, roller and plain bearings, cylinder guides, threaded spindles and worms in underwater equipment, ship’s cranes, off-shore construction elements, lifts, contact rails or distributors, clamping devices for containers or trailers, yachts, constructional parts for shipbuilding as well as finishing machines such as used in the textile and paper industry.

Suitable for all plain and roller bearings such as in water pumps, water-turbines, floodgates, escalators, spiral-toothed clutches or car-wash plants.

HIGH-LUB SW 2			12/98/21

9004372

Universal lubricant for mechanisms

exposed to saltwater atmosphere		page 2 of 3

Other forms of supply

HIGH-LUB SW 2 V

Grease dispersions for dipping or spraying. Contains white spirit acc. to VbF A II.

HIGH-LUB SW 2 SPRAY

Grease dispersion in 300 ml spray cans.

Characteristic data

Thickener				special calcium soap

Drop point			oC		approx. 110		DIN ISO 2176

Worked penetration		0,1 mm	300  15		DIN ISO 2137, p. 1

Penetration difference

after 100.000 DT		0,1 mm	max. 30		DIN ISO 2137, p. 1

Oil separation

(40 oC/18h)			%		< 1			DIN 51 817

EMCOR corrosion

test				grade		0 - 0			DIN 51 802

EMCOR corrosion

test, modified

3 % Na-Cl-solution		grade		0 - 0			DIN 51 802 modified

Tribo corrosion

surface damage				none

SRV coefficient

of friction					< 0,1

TIMKEN test								SEB 181 302

load			lbs		40

wear			mg		< 5

Four ball test			N		5000			DIN 51 350, p. 4

Salt spray test

(scratched protective

layers)

336 h/35 oC, 5 % Na Cl			no corrosion		BW-standard

HIGH-LUB SW 2			12/98/21

9004372

Universal lubricant for mechanisms

exposed to saltwater atmosphere		page 3 of 3

Combined test

sun/salt spray								BW-standard

change in weight	%		- 3,3

change in pentr.	0,1 mm	+ 37

Water resistance and							DEF-STAN

corrosion protection							91-34/1

with steel					no corrosion

This information is intended as a guide and does not necessarily represent a marketing specification. Data may vary within modest ranges but do not adversely affect the lubricant quality. Modifications reserved.