BERULUB VPN 13			12/96/21

High temperature 				9008509

antiseize compound				page 1 of 2

Description

BERULUB VPN 13 is a universal screw compound containing solid lubricants to be used for all threaded connections, particularly where high temperature or corrosive conditions cause problems.

Service temperature range:				- 30 up to + 1150°C

Consistency acc. DIN 51 818:			NLGI grade 1

To minimize the initial breakaway torque of threaded connections and to prevent corrosive seizure also at elevated temperature.

Benefits

Specially selected solid ingredients in BERULUB VPN 13 permit the lubricant to keep tightening torque tolerances very low. Consequently, overwinding or insufficient prestressing of screws is avoided.

Under appropriate flank pressure the high amount of copper powder in BERULUB VPN 13 starts forming soft films all over the thread surface. As a result, seizure - especially in the case of thread cutters - is prevented.

BERULUB VPN 13 protects mechanisms from corrosive seizure or fretting corrosion. It provides also good sealing properties and is very adhesive. BERULUB VPN 13 is lead-free.

Examples of application

To lubricate heavily loaded screws, plugged and bayonet connections of stainless steel. To help unscrew mechanisms such as furnace screws or nuts in power plants subjected to high temperature.

To seal and lubricate valves, slide valves or flat metal seals such as used in the chemical industry. To be used as a universal paste on all threaded connections in steel plants, cement plants, in ship building, mining or for agricultural machinery.

BERULUB VPN 13 is also available as BERULUB VPN 13 SPRAY in user-friendly spray cans to avoid undesirable contamination.

BERULUB VPN 13			12/96/21

High temperature				9008509

antiseize compound				page 2 of 2

Characteristic data

Thickener						gel

Unworked penetration		0,1 mm	310 - 340		DIN ISO 2137

Density 20°C				kg/dm³		approx. 1,38 		(formerly)

SEB 181 301

Water resistance					1 - 90			DIN 51 807

# Base oil

Type							synthetic oil

Kin. viscosity at 	40°C		mm²/s		approx. 350		DIN 51 562

100°C		mm²/s		approx. 50		DIN 51 562

Flash point				°C		240			DIN ISO 2592

Pourpoint				°C		approx. - 40		DIN ISO 3016

Pack size

500 ml spray can - 0,5 kg tins - 1 kg tins - 5 kg pails - 10 kg pails - 30 kg kegs

This information is intended as a guide and does not necessarily represent a marketing specification. Data may vary within modest ranges but do not adversely affect the lubricant quality. Modifications reserved.